| Vendor’s Name & Address: M/s Shoorbhoi Exports, 440 HSIIDC I.E., Barhi, Sonepat, Haryana. |  |  | Customer : Manufacturing Quality Plan Product : Screw cap socket head.& shoulder/stripper/reamer bolt. |  |  |  | P.O. No. P.O. Date : Governing specification : |  |  |  | QP No. : Rev : Date : Page 1 of 2 |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SL No. | Components | Characteristics | Class |  | Type of check | Quantum of check | Reference Document | Acceptance Norms | Format of Record |  | D* | Agency |  |  | Remarks |
|  |  |  |  |  |  |  |  |  |  |  |  | P | W | V |  |
| 1.0 | RAW | MATERIALS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 1.1 | Hot Rolled stainless steel rounds | Chemical properties |  | Major | Elements like C, Cr, Ni, Mn, Si, P etc. | One pcs per lot | AISI 410 / 420 | AISI 410/420 | Material test certificate. |  | Y | 2 | - | 1 |  |
| 2.0 | INPROCESS INSPECTION |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 2.1 2.2 | Cutting & hot Forging. MPI | Length & Dia. Before threading |  | Major Major | Dimensions MPI | As per ISO std. IS 2500-1 S.I.L S3. | As per drawing. ASTM E 709 | As per drawing ASTM E 709 | Inspection Report NDT report |  | Y Y | 2 2 | - - | 1 1 |  |
| 2.3 | Machining & Threading | Thread check. |  | Major | Dimensions & Thread check. | As per IS 2500 -1, S.I.L S3 . | As per order & drawing. | As per order & drawing | Inspection Report. |  | Y | 2 | - | 1 |  |
| 2.4 | Heat Treatment | Mech. Properties. (Hardening & Tempering) |  | Major | Tensile Strength & hardness | One per lot. | As per BHEL specs. | Conform with BHEL Specs. | Test Certificate. |  | Y | 2 | - | 1 | T.S > 800 MPa. Test sample from same lot to be tested. |
| 2.5 | Polishing | Visual |  | - | Visual | 100% | -- | -- |  | -- | - | - | - | - |  |

| LEGEND : P : Perform, W : Witness , V : Verification. Under the columns P, W & V, vendor to indicate. 1 Customer nominated Inspection Agency, 2. Vendor , 3. Sub vendor. 4. Customer’s customer/consultant as appropriate against each component/ characteristic. D* : Test certificates shall be submitted to Customer for records. ‘Y’ indicates yes. |  | Approved by Buyer’s QA Signature & Stamp. | Approved by : Buyer’s Signature & Stamp. |
| --- | --- | --- | --- |

| Vendor’s Name & Address: M/s Shoorbhoi Exports, 440 HSIIDC I.E., Barhi, Sonepat, Haryana. |  |  | Customer : Manufacturing Quality Plan Product : Screw cap socket head.& shoulder/stripper/reamer bolt. |  |  |  | P.O. No. P.O. Date : Governing specification : |  |  |  | QP No. : |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  |  |  |  | Rev : Date : |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  | Page 2 of 2. |  |  |  |  |  |  |
| SL No. | Components | Characteristics | Class |  | Type of check | Quantum of check | Reference Document | Acceptance Norms |  | Format of Record | D* | Agency |  |  |  |  | Remarks |
|  |  |  |  |  |  |  |  |  |  |  |  | P | W |  | V |  |  |
| 3 | FINAL | INSPECTION & TESTING. |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 3a 3b | Visual & dimensional inspection. Positive Material Identification for SS. | Visual & dimension check, Marking, Thread (Go – No Go). Chemical elements |  | Major Major | Dimension PMI | IS 2500-1 S.I.L S3 IS 2500-1 S.I.L S3 | BHEL spec. AISI 410 / AISI 304 | BHEL spec AISI 410 / AISI 304 |  | Inspection Report Inspection Report | Y Y | 2 3 | 1 2 |  | - 1 |  |  |
| 3c | Mechanical Properties | Tensile strength, Hardness. |  | Major | Mech. Properties | One per lot. | AISI 410 / AISI 304 | AISI 410 / AISI 304 |  | Inspection Report | Y | 3 | 2 |  | 1 |  |  |
| 3.3 | Packing | Packing |  | Major |  | 100% |  |  | P/L |  |  |  |  | 2 |  | 1 |  |

| LEGEND : P : Perform, W : Witness , V : Verification. Under the columns P, W & V, vendor to indicate. 1 Customer nominated Inspection Agency, 2. Vendor , 3. Sub vendor. 4. Customer’s customer/consultant as appropriate against each component/ characteristic. D* : Test certificates shall be submitted to Customer for records. ‘Y’ indicates yes. |  | Approved by BHEL QA Signature & Stamp. | Approved by : Customer’s Signature & Stamp. |
| --- | --- | --- | --- |