|  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Part No |  | qty |  |  | Description |  | Quantity |
| 80-077090 | | 544 |  | Heavy hex. Locknut 1"-8UNC-2B, A194-2H, zinc plated | | 544 | |
| 80-086328 | | 1424 |  | Heavy hex. Locknut 5/8"-11UNC-2B, A194-2H, zinc plated, nylon insert | | 1424 | |
| 80-091463 | | 40 |  | Heavy hex. locknut 3/4"-10UNC-2B, A194-2H, zinc plated, nylon insert | | 40 | |
| 80-086090 | | 852 |  | Heavy hex. Locknut 1 1/8"-8UN-2B, A194-2H, zinc plated, no nylon insert, ASME B18.16.6 Table 3 | | 852 | |
| 80-085190 | | 100 |  | Heavy hex. locknut 1 1/8"-8UN-2B A-194 Gr.2H Stamp Marking ASME II-A Zinc Plated, nylon insert | | 100 | |
| 80-091462 | | 100 |  | Heavy hex. locknut 1"-8UNC-2B A-194 Gr.2H Stamp marking ASME II-A Zinc Plated, nylon insert | | 100 | |
| 80-090981 | | 100 |  | Heavy hex. locknut 1 3/4"-8 UN-2B A-194 Gr.2H Stamp Marking ASME II-A Zinc Plated, nylon insert | | 100 | |
| 80-082702 | | 200 |  | Heavy hex. locknut M24 acc. to ISO 7040 or equivalent A-194 Gr.2H Stamp Marking ASME II-A Zinc Plated, nylon insert | | 200 | |
| 80-089927 | | 100 |  | Heavy hex. locknut 1 3/8"-8UN-2B A-194 Gr.2H Stamp Marking ASME II-A Zinc Plated, NYLON INSERT | | 100 | |